| Product Properties | Unit | Nominal Value |
| --- | --- | --- |
| ASTM (initial) | N/cm | 8.9 |
| PET (initial) | N/cm | 7.8 |
| PI (initial) | N/cm | 7.1 |

Packstat P587 is a translucent, double-sided non-woven tape equipped with flame retardant tackified acrylic adhesive.
This tape has especially been developed for power battery demanding mounting, lamination and converting application with flame retardant property as added value. Due to its non-flammable property, it is particularly designed to meet power battery automobile requirement.

Main Applications

- Mounting in power battery or lamination application required additional flame-retardant property.

PRODUCT BENEFIT

- Flame retardant per UL 94 VTM-0 level

- Good bonding performance

- High long-term reliability and aging resistance

- Conforming to RoHS, REACH

- Halogen-free