Main Applications

- Suitable for various types of mounting applications

- Mounting of plastic and wooden trims

- ideal for mounting of transparent signs and scales

- Mounting of decorative materials and displays

PRODUCT BENEFITS

- Excellent combination of high initial tack and immediate adhesion

- Light and aging-resistant acrylic adhesive for long-term applications

- Reliable bond even to low surface energy substrates and rough surfaces

Packstat PS 046 is a transparent, double-sided industrial mounting tape with a highly tackified adhesive and PP backing. The double-sided PP film tape is used in various industries, frequently used to mount plastic or wooden trims or fasten signs and point-of-sale displays. The tackified acrylic adhesive features excellent adhesive performance, offering a reliable bond even on low energy surfaces and rough or slightly dirty substrates. PS 046 can withstand numerous environmental factors such as humidity, UV-light and temperatures of up to 130°C for limited periods of time. The tackified acrylic adhesive makes for an excellent hold on various surfaces, very high tack, and good shear strength.

| Product Properties | Unit | Nominal Value |
| --- | --- | --- |
| Thickness | µm | 220 |
| Tensile Strength | N/cm | 50 |
| Temperature resistance long term | °C | 80 |
| Temperature resistance short term | °C | 130 |
| Adhesion to ABS Initial/After 14 days | N/cm | 12.5/14.5 |
| Adhesion to Aluminium Initial/After 14 days | N/cm | 11.5/12.5 |
| Adhesion to PC Initial/After 14 days | N/cm | 15/16.5 |
| Adhesion to PE Initial/After 14 days | N/cm | 7/8 |
| Adhesion to PET Initial/After 14 days | N/cm | 11/11.5 |
| Adhesion to PP Initial/After 14 days | N/cm | 8.5/10 |
| Adhesion to PS Initial/After 14 days | N/cm | 13/14.5 |
| Adhesion to PVC Initial/ After 14 days | N/cm | 11.5/17.5 |
| Adhesion to Steel Initial/After 14 days | N/cm | 13/13.5 |
| Colour | N/A | Transparent |